CEMENT PORTLAND  BULK CONFORMING TO ASTM C1157 TYPE-HE; WITH FOLLOWING SPECS

| Items | Units | Specification | Test Results | Test Method |
| --- | --- | --- | --- | --- |
| Chemical analysis |
| SiO2 | % | A | 22.51 | ASTM C 114 |
| Al2O3 | % | A | 5.20 |  |
| Fe2O3 | % | A | 3.05 |  |
| CaO | % | A | 59.23 |  |
| MgO | % | A | 2.40 |  |
| SO3 | % | ≤ 3.0 | 2.51 |  |
| Loss on Ignition, (LOI) | % | A | 4.00 |  |
| Insoluble Residue | % | A | 4.00 |  |
| Chloride content | % | A | 0.03 |  |
| Equi valent alkalies (Na2O+0.658 K2O) | % | A | 0.36 |  |
| Physical and Mechanical Properties |
| Finess test |  |  |  |  |
| Blaine | cm2/g | ≥ 2800 | 3950 | ASTM C 204 |
| Retained content on sieve 45(m | % | A | 1.5 | ASTM C 430 |
| Time of setting: Initial set Final set | Minutes | ≥ 45 ≤ 420 | 140 190 | ASTM C 191 |
| Heat of hydration: | KJ/kg | A |  | ASTM C 186 |
| 7 Days |  |  | 355 |  |
| 28 Days |  |  | 420 |  |
| Mass density | g/cm3 | A | 3.05 | ASTM C 188 |
| Sulfate resistance, 14 days expansion | % | A | 0.0624 | ASTM C 452 |
| Air content of mortar | % | A | 7.5 | ASTM C 185 |
| Autoclave expansion | % | ≤ 0.80 | 0.041 | ASTM C 151 |
| Compressive strength | MPa |  |  | ASTM C 109 |
| 1 Days |  | ≥ 10.0 | 15.0 |  |
| 3 Days |  | ≥ 17.0 | 21.0 |  |
| 7 Days |  | A | 25.0 |  |
| 28 Days |  | ≥ 28.0 | 35.0 |  |
| A: No applicable. |