CEMENT PORTLAND  BULK CONFORMING TO ASTM C150 TYPE-I WITH FOLLOWING SPECS

| Items | Units | Specification | Test Results | Test Method |
| --- | --- | --- | --- | --- |
| Chemical analysis |
| SiO2 | % | ≤ 22.0 | 20.51 | ASTM C 114 |
| Al2O3 | % | ≤ 5.80 | 4.92 |  |
| Fe2O3 | % | ≤ 4.00 | 3.15 |  |
| CaO | % | ≥ 59.00 | 63.66 |  |
| MgO | % | ≤ 6.00 | 1.95 |  |
| SO3 | % | ≤ 3.0 | 2.50 |  |
| Loss on Ignition, (LOI) | % | ≤ 3.00 | 2.00 |  |
| Insoluble Residue | % | ≤ 0.75 | 0.39 |  |
| Chloride content | % | A | 0.02 |  |
| Equi valent alkalies (Na2O+0.658 K2O) | % | ≤ 0.60 | 0.31 |  |
| C3S | % | A | 65.73 | BY CACULETED |
| C2S | % | A | 9.22 |  |
| C3A | % | A | 7.71 |  |
| C4AF | % | A | 9.58 |  |
| Physical and Mechanical Properties |
| Finess test |  |  |  |  |
| Blaine | cm2/g | ≥ 2800 | 3800 | ASTM C 204 |
| Retained content on sieve 45(m | % | A | 2.0 | ASTM C 430 |
| Time of setting: Initial set Final set | Minutes | ≥ 45 < 375 | 130 200 | ASTM C 191 |
| Heat of hydration: | KJ/kg | A |  | ASTM C 186 |
| 7 Days |  |  | 375 |  |
| 28 Days |  |  | 470 |  |
| Mass density | g/cm3 | A | 3.10 | ASTM C 188 |
| Sulfate resistance, 14 days expansion | % | A | 0.0704 | ASTM C 452 |
| Air content of mortar | % | ≤ 12.0 | 6.0 | ASTM C 185 |
| Autoclave expansion | % | < 0.80 | 0.032 | ASTM C 151 |
| Compressive strength | MPa |  |  | ASTM C 109 |
| 1 Days |  | A | 14.0 |  |
| 3 Days |  | ≥ 12.0 | 20.0 |  |
| 7 Days |  | ≥ 19.0 | 28.0 |  |
| 28 Days |  | ≥ 28.0 | 36.0 |  |
| A: No applicable, C3S = (4.071x%CaO)-(7.60x%SiO2)-(6.718x%Al2O3)-(1.43x%Fe2O3), C2S=(2.867) x % SiO2- (0.7544 x % C3S), C3A =(2.650x% Al2O3)-(1.692x% Fe2O3), C4AF = 3.043 x % Fe2O3 |