Certificate of quality (II)

Portland cement blended (PCB 40) or en 197-1:2000/CEM II 42.5N

or ASTM C150

Lo¹i xi m¨ng/cement			: PCB 40

Tiªu chuÈn ¸p dông/Standard		: EN 197-1:2000

Sè l«/Lot number			: Q1051

Ngµy s¶n xuÊt/Date of production	: 02 - 02 - 2013

Ngµy thö nghiÖm/Date of  testing	: 02 - 02 - 2013

| TT | tªn chØ tiªu (Characteristics) | §VT (Unit) | Yªu cÇu theo (requirements in accordance with) | kÕt qu¶ thö (results) |
| --- | --- | --- | --- | --- |
| 1 | SiO2 | % | ≤ 26 | 21.89 |
| 2 | Al2O3 | % | ≤ 6.5 | 4.76 |
| 3 | Fe2O3 | % | ≤ 4.5 | 2.84 |
| 4 | CaO | % | ≥ 54 | 61.15 |
| 5 | MgO | % | ≤ 5 | 1.45 |
| 6 | SO3 | % | ≤ 3.5 | 2.06 |
| 7 | CaOtd | % | - | 1.41 |
| 8 | Total Alkali (Na2Ot®= Na2O + 0.658 K2O) | % | ≤ 0.6 | 0.45 |
| 9 | Loss on Ignition, (LOI) | % | ≤ 10 | 3.62 |
| 10 | Insoluble Residue (IR) | % | ≤ 12 | 1.26 |
| 11 | BÒ mÆt riªng (Specific surface) | cm2/g | ≥ 3200 | 3618 |
| 12 | C­êng ®é chÞu nÐn (compressive strength) - 03 ngµy (3 days) - 28 ngµy (28 days) | N/mm2 | ≥ 42.5 | 22.2 44.8 |
| 13 | §é mÞn (Fineness) PhÇn cßn l¹i trªn sµng 0.09mm | % | ≤12 | 2.5 |
| 14 | Thêi gian ®«ng kÕt (Setting time) - B¾t ®Çu ( Initial Setting Time) - KÕt thóc (Final Setting Time) | Phót Phót | ≥45 ≤375 | 125 190 |
| 15 | §é dÎo tiªu chuÈn (Standard plasticity) | % |  | 27.75 |
| 16 | §é æn ®Þnh thÓ tÝch Le Chartelier (Soudness) | mm | ≤10 | 1.0 |

Ghi chó/Note: The remaining indicators are rechecked cement quality PCB 40 according to the EN 197-1:2000/CEM II 42.5N which is similar TCVN 6260:2009 or ASTM C150.