QUALITY OF CLINKER

Clinker in Bulk to be suitable for production of Portland cement according to ASTM C150-2a, and to comply with specifications as following:

| Items | Unit | ASTM C150-2a Specifications for OPC Type 1 |
| --- | --- | --- |
| Loss in Ignition | (%) | MAX. 3.00 |
| Insoluble Residue | (%) | MAX. 0.75 |
| SiO2 | (%) | 21.00 ÷ 22.50 |
| Al2O3 | (%) | 4.00 ÷ 6.00 |
| Fe2O3 | (%) | 2.00 ÷ 4.00 |
| CaO | (%) | MIN. 65.00 |
| MgO | (%) | MAX. 3.50 |
| SO3 | (%) | MAX. 1.0 |
| When C3A <=8% |  | MAX. 0.65 |
| When C3A > 8% |  |  |
| Equivalent Alkalis (0.658K2O + Na2O) | (%) | MAX. 0.90 |
| Free Lime | (%) | MAX. 1.00 |
| LSF |  | MIN. 93.50 |
| C3S | (%) | MIN. 52.00 |
| C2S | (%) | MAX. 28.00 |
| C3A | (%) | MIN. 6.00 |
| C4AF | (%) | MAX. 10.00 |