Quality of Clinker

The clinker to be delivered is Commercial Portland Clinker CPC 50 in bulk according Vietnam standard as per TCVN 7024 - 2002 suitable for producing Ordinary Portland Cement.

| No | Test Items | Vietnam Clinker Standard TCVN 7024 - 2002 |
| --- | --- | --- |
| 1 | SiO2 (%) | 18 - 26% |
| 2 | Al2O3 (%) | 3 - 8% |
| 3 | Fe2O3 (%) | 2 - 5 % |
| 4 | CaO (%) | 58 - 67% |
| 5 | MgO (%) | Max: 5,0% |
| 6 | SO3 (%) | Max: 1,5% |
| 7 | Free CaO (CaOtd), % | Max: 1,5%* |
| 8 | Loss on Ignition of clinker, (LOI) (%) | Max: 1,0% |
| 9 | Insoluble Residue of clinker (%) | Max: 0,75% |
|  | C3S (%) | Min: 54% |
|  | C2S (%) | 12 - 20 |
|  | C3A (%) | 7 - 12 |
|  | C4AF (%) | 7 - 12 |
|  | LSF | Min: 92 |
|  | Grain size: 0 - 1mm 5 - 25mm | Max: 10% Min: 40% |
|  | Compressive Strength, Mpa 3 days of CPC 50 | Min: 28N/mm2 |
|  | Moisture of clinker (%) | Max: 1% |